Automated On-Sun Analysis
Including module modeling and flux map characterization

---
Module Inputs
- Calibration Constants/Experimental Config
- Flux Map
  - Module ART (spatial)
- Module Design
  - Optical Stack ART
  - Design characteristics
- Experimental Results

---
Calibration Constants:
Directly In Code
- masking = 0.35
- shading = 0.08 #on dish from receiver
- mirror_loss = 0.11
- #Calibration constants
- PV_flow_cal = (20/3-2/6)/(5)
- TR_flow_cal = 200/(5*60)
- PV_pres_cal = 15/0.12
- GHI_cal = 5000
- DNI_cal = 0.00000776
- Cp_water = 4.184
- TR fraction = 0.57 #open area after CPV before receiver, estimated
- TR efficiency = 0.95
- CPV_mismatch = 0.085
- Module Series Resistance = 0.126 Ohms
- Cell_area = 0.0055**2

---
Flux Map:
Modeling/Flux_Maps
58.5_844 DNI
- Run with: OpticalFluxChar.py
- Inputs
  - Flux maps
    - 58.5_844DNI.xlsx (Mod 5, 6 position)
    - 65.0_515DNI.csv (Mod 7+ position)
  - Aperture Size
  - Module ART (optional)
- Outputs:
  - Flux maps (visual)
  - Concentration maps (text)
  - Module Spatial ART
Module 6 Spatial ART
	Cell	Bypass	Bypass w/Ch
Absorption	0.6345	0.0491	0.0666
Reflection	0.2445	0.0662	0.0808
Transmission	0.121	0.8847	0.8526
Mod6_58.5 Spatial ART
	Bypass No Chan	Bypass Chan	Cells	Total
Power	0.4329	0.2078	0.3592	1
A	0.0212	0.0138	0.2279	0.2630
R	0.0286	0.0167	0.0878	0.1332
T	0.3829	0.1772	0.0434	0.6036

---
Module Design
Modeling/Module_Properties
- Run with: CPVPerformance.py
- Input
  - Cell ART
  - Cell Eff (hardcoded at 22% from John’s calc.)
  - Module Design (encap thickness, cells, etc.)
- Outputs
  - Temp Maps
  - Heat fraction
  - Elec. Fraction
  - Thermal Restiance

---
Experimental Results
Test_Data
- Data Logger Header
- Data Logger – Temperatures, Pressures, DNI
- IV sweep data
- IV sweep stats
- MPP data
Following data shows the analysis of Mod6 Tests done on 1-23-18 using the 58.5_844DNI flux map

---
Outputs: Power flow analysis
	Exp	Model	%delta
PV Cooling	55.61	57.24	-2%
PV Power	15.63	23.94	-34%
Reflection	76.8	72.98	5%
Transmitted	202	228	-11%

---
Cell Temperature
Predicted Temperatures
        Loc. Conc.	Temp (degC)
PV TC1 AB22	492	71.61
PV TC2 BC66	445	70.54
PV TC3 FG55	531	76.695
Avg	None	459	71.6188

---
Thermal Resistance Calculation
Plots available for all other TCs as well
	Conc.	Morn	Std err	Afternoon	Std err
Avg	459	2.2	0.07	5.6	0.04
PV TC1	492	1.6	0.11	7.09	0.063
PV TC2	445	0.45	0.08	2.92	0.045
PV TC5	531	3.8	0.14	5.6	0.91

---
Updates
- Easy
  - Comparison of Thermal Resistance
  - Comparison of Temperatures
  - Jsc vs DNI plots
- Slightly Harder
  - Electrical characterization

---
Data to Check
- Cell ART - Vera
- Mod ART - Vera

---
Mod 6 Cell ART
	Air-N-BK7	N-BK7-Silicone	Silicone-Solar cell	Solar cell-Silicone	Silicone-Sapphire	Sapphire-Water	Water-N-BK7	N-BK7-Air
In-band T	0.9651	0.9648	0.8733	0	0	0	0	0
Out-of-band T	0.9665	0.9662	0.8255	0.6772	0.6764	0.6658	0.6397	0.6228
Total T	0.9656	0.9653	0.8574	0.2264	0.2261	0.2226	0.2138	0.2082
In-band R	0.0349	0.0352	0.1241	0.1241	0.1241	0.1241	0.1241	0.1241
Out-of-band R	0.0335	0.0338	0.1697	0.2	0.2007	0.2103	0.2112	0.2262
Total R	0.0344	0.0347	0.1393	0.1495	0.1497	0.1529	0.1532	0.1582
In-band A	0	0	0.0026	0.8759	0.8759	0.8759	0.8759	0.8759
Out-of-band A	0	0	0.0048	0.1228	0.1229	0.1238	0.149	0.1509
Total A	0	0	0.0033	0.6242	0.6242	0.6245	0.6329	0.6336
Inband A	0	0	0.0026	0.8733	0	0	0	0
outofband A	0	0	0.0048	0.118	0.0001	0.001	0.0252	0.0019
total A	0	0	0.0033	0.6209	0	0.0003	0.0084	0.0006

---
Module 6 ART
Module 6 Spatial ART
	Cell	Bypass	Bypass w/Ch
Absorption	0.6345	0.0491	0.0666
Reflection	0.2445	0.0662	0.0808
Transmission	0.121	0.8847	0.8526